#129 Channel Slot Triangular Wire Tie

SECTION 04 00 00 MASONRY

Section 04 05 19.16 Masonry Anchors

Section 04 05 23 Masonry Accessories

PART 1: GENERAL

1.1 RELATED SECTIONS

A. Provide shop drawings for all product locations.

1.2 SUBMITTALS

A. Manufacturer Certificate of Compliance for materials.

B. Product Data: Manufacturer’s data sheet on each type of product 					    furnished.

PART 2: MANUFACTURER

2.1 MANUFACTURER

Heckmann Building Products

110 Richards Ave.

Norwalk, CT 06854-1685

800-621-4140

Email: info@heckmannanchors.com

Website:  www.heckmannanchors.com

2.2 APPLICATIONS

A. Provide anchoring systems that comply with the Building Code Requirements 	for Masonry Structures TMS 402-16.

B. ASTM A 36/A36M-14 Standard Specification for Carbon Structural Steel.

C. ASTM A1008/A1008M Sheet Metal Anchors and Ties (Plain Steel)

D. ASTM A153/A153M-16 Standard Specification for Zinc Coating (Hot-Dip) on 	Iron and Steel Hardware

E. Stainless Steel AISI [Type 304]

F. ASTM A240/A240M-15b Standard Specification for Chromium and Chromium-	Nickel Stainless Steel Plate, Sheet, and Strip for Pressure Vessels and for 	General Application.

G. ASTM A580/A580M-15 Standard Specification for Stainless Steel Wire

H. ASTM A666-15 Standard Specification for Annealed or Cold-Worked 	Austenitic Stainless Steel Sheet, Strip, Plate, and Flat Bar.

2.3 MATERIALS

For Use with channel slots:

Select the Folowing

129 CHANNEL SLOT TRIANGULAR WIRE TIE

12 gage clip factory assembled to a 3/16 inch (4.76 mm) diameter x [3”] [4”] [5”] [6”] [7”] [9”]

Materials: [Hotdip Galvanized After Fabrication] [Stainless Steel]

PART 3: EXECUTION

A. Install as specified in applicable masonry section(s).