#187 Hole-Type Brick Veneer Anchor

SECTION 04 00 00 MASONRY

Section 04 05 19.16 Masonry Anchors

Section 04 05 23 Masonry Accessories

**PART 1: GENERAL**

 1.1 RELATED SECTIONS

 A. Provide shop drawings for all product locations.

 1.2 SUBMITTALS

 A. Manufacturer Certificate of Compliance for materials.

 B. Product Data: Manufacturer’s data sheet on each type of product furnished.

**PART 2: MANUFACTURER**

 2.1 MANUFACTURER

 Heckmann Building Products

 110 Richards Ave.

 Norwalk, CT 06854-1685

 800-621-4140

 Email: info@heckmannanchors.com

 Website: [www.heckmannanchors.com](http://www.heckmannanchors.com)

2.2 APPLICATIONS

1. Provide anchoring systems that comply with the Building Code Requirements for Masonry Structures TMS 402-22.
2. Stainless Steel AISI [Type 304] or [Type 316].
3. ASTM A240/A240M-15b Standard Specification for Chromium and Chromium Nickel Stainless Steel Plate, Sheet, and Strip for Pressure Vessels and for General Application.
4. ASTM A666-15 Standard Specification for Annealed or Cold-Worked Austenitic Stainless Steel Sheet, Strip, Plate, and Flat Bar.
5. ASTM A153/A153M-16 Standard Specification for Zinc Coating (Hot-Dip) on Iron and Steel Hardware.
6. Zinc Alloy 710 for use as a firewall anchor (1/8” thick only).
	1. MATERIALS

***Select the Following***

**187 HOLE-TYPE BRICK VENEER ANCHOR**

**Standard:** 16 gauge x 1-1/4” wide with a 1-1/2” od bend with a centered 5/16” diameter hole. Length: [3-1/2”] [5-1/2”] Steel Type: [Type 304 Stainless Steel] [Hotdip Galvanized After Fabrication] [Zinc Alloy710 for Firewall Applications]

**Custom:** (For custom sizes refer to product 340-A Corrugated L-Anchor with Hole)

**PART 3: EXECUTION**

 A. Install as specified in applicable masonry section(s).